2008 Annual Report

Chemical Durability and Analysis (TC No.2)

Chairman: 	Dominique Brochot, Corning SAS CETC, Avon, France

Vice-Chair:	Maria Malheiro, Saint-Gobain Recherche, Aubervilliers, France

Secretary :	Peter Sundberg, Glafo, Vaxjo, Sweden

Members:	Ryouji Akiyama, Asahi glass, Yokohama, Japan

Ayse Kerestecioglu, Sisecam, Istanbul, Turkey

Andreas Kasper & Elke Chorus, Saint-Gobain Deutschland, Herzogenrath, Germany

Martina Scarpa, Stazione Sper. Vetro, Venezia, Italy

Leos Bauer, Glass Institute, Hradec Kralove, Czech Republic

Isabelle Lesieur, Isover Saint-Gobain, Rantigny, France

Maria Malheiro, Saint-Gobain Recherche, Aubervilliers, France

Heinrich Kipphardt, BAM, Berlin, Germany

Ralf Eiden & Christine Strubel, Schott, Mainz, Germany

Dominique Michiels, Glaverbel, Jumet, Belgium

Carolina Brillante, Filippine

Scott Clemons, Corning INC, Corning,NY, USA

José Simons, INISMa, Charleroi, Belgium

Stuart Jamieson, Pilkington plc, Lathom, UK

Daniel Capon, GTS, Sheffield, UK

Tepiwan Jitwatcharakomol, Glass Tech Center. Bangkok, Thailand

Hon. Members :

Emanuel Guadagnino

Orhan Corumluoglu

SUMMARY

Membership:  Dr Maria Malheiro is now appointed vice-chairman, replacing Dr Peter Sundberg. Ayse Kerestecioglu (Sisecam) replaces Ilkay Sökmen and Dr Heinrich Kipphardt replaces Dr Matschat ( BAM ).

Many new members have joined or are joining the group this year : Dr Tepiwan Jitwatcharakomol ( Tech Glass Center in Bangkok ), Dr Tatiana Antropova (Institute Silicate Chemistry, St. Petersburg),  Dr Sjaak Smolders ( Philips Research Europe, Eindhoven ).

Meetings: TC2 met twice in 2008, in Corning ( US ) on May 15-16 (8 members in attendance) and in Aachen ( Germany ) on October 23-24 (14 people).

Two core meetings have been held in Avon ( February 02 and October 13 ) with respectively 3 and 4 members in attendance.

Activity: Collaborative works have been successfully closed (SGT sand, slag), some others need to be continued next year (Surface Ablation Cell in comparison with other techniques, sulphur/sulphides in an amber glass ) and new ones were initiated

( N, C, S in AZS refractories in collaboration with TC11 and TC14, iron in low iron glass sand and low iron float glass ).

Communication : papers presented at the Strasbourg workshop have been published on the Revista SSV ( EFONGA fundings ), the “Handbook of Analytical Methods recommended by TC2” will be soon printed and the paper on SAC results will be published in Glass Technology in the next months. A great news : our TC2 website is launched !

PLANS AND DELIVERABLES FOR 2008

- Surface Ablation Cell : first paper to be published, comparison with other techniques in progress.

- Proficiency test on Slag : ended : certificates to participants distributed

- Sand analysis ( collaboration with SGT ) : certification completed.

- Sulphur/Sulphides in an amber glass : first results discussed. More work needed.

- Handbook of Analytical Methods recommended by TC2 : to be print before end of year

- 2 meetings and 2 core meetings held : documents issued

- TC2 website launched

# ACTIVITIES in 2008

TC2 met first in Corning ( NY ) in May 2008 hosted by Corning Inc. Following topics were discussed :

- Report on EFONGA activities

- “Handbook of Analytical Methods recommended by TC2” compiled by Emanuel Guadagnino and Orhan Corumluoglu ( choice of methods, common format )

- Revision of ISO 4802 ( Hydrolytic Resistance of the interior surface of glass container : Italian comments discussed

- Certification of SGT sand : work completed. Sand available from SGT.

- SAC : results of 3 labs presented. Comparison with SIMS technique correlates perfectly ( see B and Sn profiles )

- Proficiency test on Slag : choice of sample, homogeneity test discussed.

- Sulphur/sulphide in amber glass : identification and distribution of the glass.

- LIBS : presentations and uses of the technique made by Corning and Pilkington.

- Collaboration with TC11 and TC14 for the determination of C, N and S in AZS refractories : understanding of the demand.

- Vitroceramic sample for certification : to be check by Corning and Schott

- Determination of main components in BAM S005

- Mercury in glass : need for a reference material to show labs ability.

TC2 met again in Aachen  in October, hosted by Sekurit Saint Gobain

The following issues were discussed :

- Report on CTC meeting in Trencin

- Revision of ISO 4802 : Emanuel Guadagnino invited to Berlin’s meetings in November.

- Roadmap questionnaire : inputs of the group received and forwarded to Joachim Klemens

- Small presentation of EFONGA and GlaSS project  to our new members

- “Handbook of Analytical methods recommended by TC2” : presentation of the chosen methods under a new format. Printing in progress.

- TC2 website : presentation by Peter Sundberg of the potentialities of this tool.

- Proficiency test on Slag : discussion of results and distribution of participating certificates.

- Sulphur/Sulphide in amber glass : presentation of the results. As the sulphides results are too spread, it has been decided to focus on methods that give best results and make new trials with those methods.

- Presentations of surface studies on borofloat using LA ICPMS made by BAM and Schott.

- SAC : presentation of the results obtained by the 3 laboratories and of the draft paper for publication. Improvements discussed.

- N, C and S in AZS refractories : Dr Detlef Köpsel presented its request concerning impurities analysis in AZS refratories. It was decided to investigate with different techniques (LECO,  HR GDMS, SIMS, LA ICPMS)

- Main elements in BAM S005 : search for left glass pieces to allow labs without XRF equipment to participate to this exercise.

- New topics were discussed : iron in a low iron glass sand and in a low iron float glass.

- Decision for next meeting : Pilkington invites us in Lathom ( UK ) in April 2009.

Main documents issued :

ICG/TC2/08-1469 : Minutes of core meeting / Avon February 2008

ICG/TC2/08-1484 : Report from the 89th meeting / Corning May 2008

ICG/TC2/08-1488 : LIBS presentation by Corning US

ICG/TC2/08-1494 : LIBS for cullet sorting ( Pilkington )

ICG/TC2/08-1494 : Minutes of core meeting / Avon October 2008

ICG/TC2/08-1496 : SO3 in glass by combustion/final manuscript

ICG/TC2/08-1500 : Report from the 90th meeting / Aachen October 2008

ICG/TC2/08-1501 : Action sheet arising from the 90th meeting in Aachen

PLANS FOR 2009 AND DELIVERABLES

( EFONGA activity:

- “Surface Ablation Cell” ( SAC ): some more additional work will be done before submitting the final paper to Glass Technology

- LA ICPMS studies on Borofloat CS2007-1 glass ( comparison with SAC results )

- Sulphur/sulphides in an amber glass : new trials to be done on sulphides determination using ICP OES and titration methods ( working methods )

- In collaboration with TC11 and TC14, determination of C, S and N in AZS refractories ( trials with LECO, LA ICPMS, SIMS and HR GDMS )

- Proficiency tests on iron determinations in low iron glass sand and low iron float glass.

- Determination of main components of BAM005S ( previously investigated for impurities )

- Spring meeting will be held in Lathom ( UK ) at the invitation of Pilkington.

- Fall meeting : place to be discussed.

PUBLICATIONS AND OTHER CONTRIBUTIONS

- E.Guadagnino, D. Brochot & P.Sundberg : "ICG-TC2 expriences in collaborative studies, method validation and proficiency testing", Riv. Staz. Sper. Vetro, 6, 2007, 5-11

- U. Waetjien, E.Guadagnino :  "How and why to certify reference materials", Riv. Staz. Sper. Vetro, 6, 2007, 13-18

- H. Kipphardt,  R.Matschat  : "Traceability and uncertainty of chemical measurements in the frame of the certification and use of the glass CRM BAM- S005", Riv. Staz. Sper. Vetro, 6, 2007, 19-23